|  |  |
| --- | --- |
|  | **AKross Premium Progress 5W-40 SL/CF** |

|  |  |
| --- | --- |
|  | **PERFORMANCES LEVELS****API** SL/CF**SAE** 5W-40**ACEA** A3/B4**DESCRIPTION**AKross Premium Progress 5w 40 SL/CF is a universal, multigrade, syntatic oil. It is made on a high-quality syntatic base oil and multifunctional foreign addictives. The oil possesses stable viscosity and temperature properties that protect engine from wear and corrosion. |

|  |
| --- |
| **APPLICATIONS**The motor oil AKross PREMIUM PROGRESS 5W-30 SL/CF is intended for modern high-performace gasoline and diesel engines of cars, trucks, vans, that require the use of API SL/CF lubricants. |
| **PACKAGING**All products are produced in plastic canisters 1L, 4L, 5L and in steel barrels 205L. |
| **PROPERTIES AND SPECIFICATIONS**

|  |  |  |
| --- | --- | --- |
| **Properties** | **Method** | **Value** |
| Kinematic Viscosity at 100°С, mm2/s | ASTM D445 | 14,0 |
| Viscosity Index | ASTM D97 | 168 |
| Flash Point, °С | ASTM D92 | 211 |
| Density at 20°С, kg/m3 | ASTM D 1298 | 856 |
| Pour Point, °С | ASTM D97 | -37 |
| Perchloric acid, mg KOH/g | ASTM D4739 | 6,5 |
| Sulphated ash, wt % | ASTM D874 | 1,2 |
| The features mentioned above are average values obtained with some variability in production and do not constitute a specification. |

 |
|  |