|  |  |
| --- | --- |
|  | **AKross Premium Progress 5W-40 SL/CF** |

|  |  |
| --- | --- |
|  | **PERFORMANCES LEVELS**  **API** SL/CF **SAE** 5W-40 **ACEA** A3/B4  **DESCRIPTION**  AKross Premium Progress 5w 40 SL/CF is a universal, multigrade, syntatic oil. It is made on a high-quality syntatic base oil and multifunctional foreign addictives.  The oil possesses stable viscosity and temperature properties that protect engine from wear and corrosion. |

|  |
| --- |
| **APPLICATIONS**  The motor oil AKross PREMIUM PROGRESS 5W-30 SL/CF is intended for modern high-performace gasoline and diesel engines of cars, trucks, vans, that require the use of API SL/CF lubricants. |
| **PACKAGING**  All products are produced in plastic canisters 1L, 4L, 5L and in steel barrels 205L. |
| **PROPERTIES AND SPECIFICATIONS**   |  |  |  | | --- | --- | --- | | **Properties** | **Method** | **Value** | | Kinematic Viscosity at 100°С, mm2/s | ASTM D445 | 14,0 | | Viscosity Index | ASTM D97 | 168 | | Flash Point, °С | ASTM D92 | 211 | | Density at 20°С, kg/m3 | ASTM D 1298 | 856 | | Pour Point, °С | ASTM D97 | -37 | | Perchloric acid, mg KOH/g | ASTM D4739 | 6,5 | | Sulphated ash, wt % | ASTM D874 | 1,2 | | The features mentioned above are average values obtained with some variability in production and do not constitute a specification. | | | |
|  |